## Slide 1
AC Corrosion During Construction
  Mark Anderson – Sr Project Manager
  Western Region Gas Conference
  August 20, 2025

## Slide 2: Pipeline Route
80 miles, 12 - inch OD, steel, Fusion Bonded Epoxy pipeline

## Slide 3: ILI MFL Tool Run
Tool ran
Hundreds of exterior metal loss features reported

## Slide 4: ILI External Metal Loss
Chart: % Wall loss depth

## Slide 5: Typical Dig Site

## Slide 6: Typical Dig Site (Day Light Pipe at Anomaly)

## Slide 7: Typical Dig Site (Verify Location and Take Initial Readings)

## Slide 8: Typical Dig Site (Evaluate Corrosion Product)

## Slide 9: Typical Dig Site (Evaluate Coating and Take pH Readings at Anomaly

## Slide 10: Typical Dig Site (Expose Pipe 360 deg)
Zinc Ribbon-
Installed over the
Pipeline

## Slide 11: Typical Dig Site (Coating Evaluation)
Note on Pipe from Original Construction - “Jeep”

## Slide 12: Typical Dig Site (Anomaly Cleaned for Final Measurements)

## Slide 13: Metal Loss at Long Seam

## Slide 14: Metal Loss at Girth Weld

## Slide 15: Metal Loss Around Pipe (Maybe Gouge / Turned into AC Corrosion)

## Slide 16: Cathodic disbondment

## Slide 17: Summary of Field Evaluation
25 External Metal Loss Indications exposed
  All 25 metal loss indications were caused by AC corrosion
  AC Current Density measured with AC-10 portable density prob
    Highest reading was 0.1 A/m2
  pH of pipe at metal loss, all 9+
  Soil Resistivity ranged from 300 to 700 Ωcm, average was 544 Ωcm

## Slide 18: AC Model (Pre-Construction)
Note: 2.8 A/sq.ft – Lower threshold for AC corrosion – 30 A/sq.m
9.29 A/sq.ft – Upper threshold for AC corrosion – 100 A/sq.m

## Slide 19: Installation of AC Mitigation System
Zinc ribbon along 60 miles of the route, total of 600,000 ft of zinc ribbon installed.
85 each solid state decouplers installed along the route

## Slide 20: Installation of AC Mitigation System

## Slide 21: AC Volts
Chart: AC Volts at TS 2 ½ Years After Start of Construction


## Slide 22: AC Volts
Chart: Present - AC Volts

## Slide 23: AC Current Density
Chart: Present Day AC Current Density

## Slide 24: Questions Asked
  Why was there so many metal loss anomalies caused by AC corrosion?
  Is the AC corrosion active? - NO
  What mitigative action should be taken?

## Slide 25: Corrosion Growth Rate
Total wall loss in mils / duration of active wall loss in years
Example:
85 mils of metal loss over a 10-year period –
85 mills/10 years = 8.5 mils per year

## Slide 26: Corrosion Growth Rate
Adequate CP is a corrosion growth rate of less than 1 mil per year
  NACE SP0169
  Section 6: Criteria and Other Considerations for Cathodic Protection,
  6.1 Introduction …..A commonly used benchmark for effective external corrosion control is (a reduction in the corrosion rate to 0.025 mm per year (1 mil per year) or less.
Maximum galvanic corrosion is 16 mil per year
  NACE SP0502
  Appendix C
  C 2 Default Corrion Rate
  C3,2 When other data are not available, a pitting rate of 0.4 mm/y (16 mpy) should be used for determining reinspection intervals.

## Slide 27: Corrosion Growth Rate
We needed to establish how long AC corrosion was active

## Slide 28: Timeline
Timeline:
Construction started - AC Corrosion Start
Hydrostatic Test – .75 years
DCVG - 1 year
CIS Survey ON/OFF - 1.5 years
VAC at TS, highest reading was 4.114 Volts - 2.5 years
ILI – 6.5 years

## Slide 29: Installation of AC Mitigation System
Zinc ribbon was installed as pipeline was laid.
Decoupler were commissioned after hydrostatic test.

## Slide 30: DCVG Indications Summary
Total of 503 Indications
%IR
  6% and greater - 0
  5% - 1
  4% - 1
  3% - 1
  2% - 11
  1% - 489

## Slide 31: Decoupler Effect on ON/OFF Survey
Figures from DAIRYLAND Industry publication-
Testing and Evaluation of Decoupler Capacitive Effects and Utilization of the Dairyland Model PCRX | Published October 6, 2020
Normal Wave Form
Wave Form of Pipeline being
Effected by Decouplers

## Slide 32: Wave Form at Various Interruption Cycles
14 wave forms at different ON/OFF cycles were taken

## Slide 33: Current TP Survey vs Original CIS
Chart: Volts DC ON/OFF
| 747 | 5903 | 15040 | 23930 | 32464 | 40263 | 43496 | 53774 | 59176 | 64402 | 70037 | 74811 | 79685 | 85775 | 93861 | 100805 | 108834 | 114043 | 120348 | 129603 | 143343 | 156395 | 162690 | 170216 | 177747 | 183247 | 194468 | 212817 | 220854 | 233890 | 242751 | 251429 | 261240 | 269147 | 276603 | 291400 | 301139 | 326839 | 347393 | 355160 | 367362 | 385469 | 424389
ON | 1.726 | 1.536 | 1.556 | 1.486 | 1.382 | 1.315 | 1.369 | 1.357 | 1.349 | 1.333 | 1.268 | 1.376 | 1.361 | 1.493 | 1.592 | 1.638 | 1.547 | 1.545 | 1.838 | 1.353 | 1.444 | 1.387 | 1.359 | 1.3 | 1.233 | 1.167 | 1.219 | 1.259 | 1.269 | 1.429 | 1.496 | 1.519 | 1.655 | 1.598 | 1.602 | 1.567 | 1.584 | 1.518 | 1.566 | 1.563 | 1.55 | 1.518 | 1.971
OFF | 0.914 | 0.781 | 0.976 | 0.981 | 0.938 | 0.899 | 0.971 | 0.849 | 0.868 | 0.879 | 0.863 | 0.913 | 0.869 | 0.957 | 1.009 | 1.017 | 0.906 | 0.926 | 1.265 | 0.809 | 0.972 | 0.951 | 0.949 | 0.916 | 0.867 | 0.846 | 0.891 | 0.876 | 0.882 | 0.918 | 0.92 | 0.914 | 0.939 | 0.947 | 0.984 | 1.006 | 1.048 | 1.042 | 1.134 | 1.14 | 1.161 | 1.11 | 1.469
-0.85 | 0.85 | 0.85
Rectifiers | 0.7 | 0.7 | 0.7 | 0.7
Original CIS Summary:
No OFF Readings less
Negative than -0.850 VDC

## Slide 34: Original CIS vs Current CIS
Current CIS
Original CIS

## Slide 35: Questions Asked
  Why was there so many metal loss anomalies caused by AC corrosion? –
  AC Mitigation System Was Not Operational When Pipe Was Put in Ground
  Is the AC corrosion active? - NO
  What mitigative action should be taken?

## Slide 36: Corrosion Growth
 |  | Mils per Year | 
Activity | Duration Years | 70% | 50%
Start Construction |  |  | 
Hydro Test | 0.75 | 0.311 | 0.226
AC Mitigation System Put in Service | 1.00 | 0.233 | 0.170
ILI | 6.50 | 0.036 | 0.026

## Slide 37: Questions Asked
  Why was there so many metal loss anomalies caused by AC corrosion?
  No AC Mitigation System Operational When Pipe Was Put in Ground
  Is the AC corrosion active? - NO
  What is the expected life of the pipeline? –
  Less than 1 year if AC is not mitigated
  What mitigative action should be taken? – Active Monitoring

## Slide 38: Active Monitoring

## Slide 39: Summary
  AC corrosion starts as soon as the pipe is buried
  AC mitigation is not active until system is commissioned
  Plan on AC mitigation as the pipe is buried (maybe temporary)
  Metal loss due to AC corrosion can be magnitudes greater than galvanic corrosion

## Slide 40
Thank You!
Mark Anderson
manderson@entrustsol.com