## Slide 1: Advancements in Failure Analysis, Laboratory Testing and Artificial Intelligence
Laboratory Services
Aaron Mee
Greg Efthemes

## Slide 2: Technology in the Lab
With the advent of artificial intelligence (AI), testing appliances and processes are making quantum leaps forward before our eyes.
Subsequently, technology and techniques for materials testing and material investigations are developing rapidly.
Characterization, Analysis and Data Management

## Slide 3: AI Vernacular
Agenetic AI (AI Gentics) - Study and development of intelligent agents that can operate autonomously and make decisions based on their environment. Now
Generative AI - focused on creating new content, such as images, text, music, or other media, based on patterns learned from existing data. Now
Robots – first generation autonomous ~$80K, FY26-27

## Slide 4: Four Types of AI
Reactive Machines: capable of reacting to situations based on predefined rules and inputs. No memory or ability to learn. Chess Playing program can only respond to opponents moves.
Limited Memory: learn from past experiences and use that knowledge to make better decisions in the future. Self driving cars.
Theory of Mind: advanced and aims to understand human emotions, beliefs, and intentions. It goes beyond simply reacting to inputs and tries to grasp the "why.” Honking horn = likely impatient person.
Self-Aware: most advanced and hypothetical type of AI. Self-aware AI would possess consciousness, self-awareness, and the ability to understand its own internal states. Theoretical and yet to be realized.

## Slide 5
Scaling Laws have been Deciphered: data and math to achieve the next level AI is now known.
Think Time: allowed AI to run inferential computations to calculate scaling scenarios.
Mastered Distillation: one AI teaches the next generation AI; the student becomes exponentially smarter than the teacher “evolution in fast forward.”
Each generation of AI will grow in unfathomable orders of magnitude form the previous generation.
Three Stages of AI – Development Pattern

## Slide 6
GPT’s Exponential Growth – Orders of Magnitude
GPT-1 (2018): 102 - 117 million additional parameters.
GPT-2 (2019): 109 - 1.5 billion additional parameters.
GPT-3 (2020): 1011 – 175 billion additional parameters.
GPT-4 (2023): 1012 – 1.76 trillion additional parameters (~10x GPT-3).
*GPT-4.5 (2025): 1013 - 2.00 trillion+ additional parameters (mainly an architectural refinement & optimization for GPT 5 capacity).
*GPT-5 (2025): 1014 - projected 4-5 trillion additional parameters.

## Slide 7: AI in the Lab
AI Products:
    GPT 3, 4 4.5 & 5: exceptionally broad bandwidth, understanding the ask, low error rate, problem solving.
    Gemini – good with Google ecosystem & long context reasoning.
    Grok - humor, casual use, and real-time insights (by X).
    DeepSeek: multimodal analysis, complex reasoning, strategic planning; Chinese owned, Open AI distilled, banned in 9 states.
    Claude: safety, ethical considerations, and detailed, nuanced reasoning; good for coding.
    Chat on AI: powered by GPT, image generation, web search, document processing

## Slide 8: AI Case Study I
Creating an Email in MS Outlook using an Excel Spreadsheet to Extract Failure Analysis Database Details

## Slide 9
Excel Visual Basic for Applications (VBA) Task Automation Screenshot
ChatGPT
Thinking…
Excel macros once took hours of VBA study,
Followed by hours of trial and error.
Today, they are a few questions away.

## Slide 10
End Result
ALT + F8

## Slide 11: AI Case Study II
Teaching AI to Read Electrofusion Coupling Digital X-Rays
A Joint Research Project

## Slide 12
Transforming Electrofusion Joint Inspection with AI
Sand Contamination Detected

## Slide 13
Transforming Electrofusion Joint Inspection with AI
NYSEARCH, along with Southwest Gas and peer utilities, is piloting AI, from Cogniac, to flag EF joint defects.
Utility SMEs annotated EF X-rays.
  Models were trained to detect sand, wire-walk, short stab, and similar anomalies.

## Slide 14
Transforming Electrofusion Joint Inspection with AI
Training Methodologies
Area Model Training
Box Model Training
Exact defect pixels traced.
Pro: More precise. Con: Slower to label
- Boxes are drawn around defects. - Pro: Quicker to label. - Con: Less precise.

## Slide 15
Box Model Training

## Slide 16
Area Model Training

## Slide 17
Transforming Electrofusion Joint Inspection with AI
Once trained, the models achieved fast & consistent pass/fail guidance, regardless of training methodology
Image recognition software trained with the area detection methodology was able to predict sand contamination 86% of the time.
  These early results are outstanding given the prevalence of human error in X-ray interpretation, and the limited amount of training media provided to the models thus far.

## Slide 18
Transforming Electrofusion Joint Inspection with AI
Cogniac experts will continue working with utility SMEs to fine-tune models for even higher success rates.
Further field testing with Utility SMEs will validate these advances in real-world conditions.
AI model accuracy and reliability will continue to improve with each x-ray image submitted to the dataset.
Utilities may soon be able to upload X-ray images to Cogniac and get rapid, objective pass/fail results.
New Developments

## Slide 19: Digital Radiography in the Lab
Golden Engineering: XRS3 GFX 20V Portable X-ray
Is AI Interpretation a Bridge too Far?

## Slide 20
Wall Loss – Pitting or Mill Scale

## Slide 21: AI Case Study III
Residential Meters with an Insert Issue: Statistical Lot Inspection

## Slide 22: Quarantine: Residential Gas Meter Insert Issue
The manufacturer reported their meters had a series of inserts (spuds) breaking before installation.
22,000 meters with 17,700 initially quarantined.
While affected lot numbers were available to quarantine, additional inspection was needed to achieve a LOC for the remaining lots.

## Slide 24
Hypergeometric Probability Distribution |  |  |  |  | 
Xxxx – Residential Meters |  |  |  |  | 
Sample Size by Batch Size Table |  |  |  |  | 
Assuming the following: |  |  |  |  | 
100,000 units (meters with a singular component potentially affected) |  |  |  |  | 
Estimated Proportion of Defectives (p): 0.3333 |  |  |  |  | 
95% Confidence Level |  |  |  |  | 
Batch Size | Number of Fittings per Batch | Sample Size (E=0.01) | Sample Size (E=0.02) | Sample Size (E=0.03) | Sample Size (E=0.05)
5 | 5 | 5 | 4 | 3 | 2
10 | 10 | 6 | 5 | 3 | 2
15 | 15 | 7 | 6 | 3 | 2
20 | 20 | 8 | 6 | 4 | 2
25 | 25 | 9 | 7 | 4 | 2
50 | 50 | 12 | 8 | 5 | 3
75 | 75 | 14 | 9 | 6 | 4
100 | 100 | 17 | 11 | 7 | 4
250 | 250 | 28 | 14 | 9 | 5
500 | 500 | 39 | 19 | 12 | 7
750 | 750 | 47 | 23 | 15 | 9
1,000 | 1,000 | 56 | 27 | 17 | 10
Explanation of the Table: |  |  |  |  |  | 
Batch Size: The total number of fittings in each box or batch. |  |  |  |  |  | 
Sample Size: The number of fittings that should be inspected based on different margins of error, calculated as a proportion of the fittings in each batch. |  |  |  |  |  | 
Examples: |  |  |  |  |  | 
1. If there is a box with 25 fittings: |  |  |  |  |  | 
 | For E = 2%: Sample Size = 7 fittings should be inspected. |  |  |  |  | 
 | For E = 5%: Sample Size = 2 fitting should be inspected. |  |  |  |  | 
2. If a location has 30 boxes, each containing 25 fittings: |  |  |  |  |  | 
 | Total fittings: 30 boxes × 25 fittings/box = 750 fittings. |  |  |  |  | 
 | For E = 2%: Recommended Sample Size = 4 fittings per box × 30 boxes = 120 fittings should be inspected. |  |  |  |  | 
 | For E = 5%: Recommended Sample Size = 1 fitting per box × 30 boxes = 30 fittings should be inspected. |  |  |  |  | 

## Slide 25: UT Instruments and Scanning
USM100, MENTOR UT FLAW DETECTION
COMPACT PAUT

## Slide 27: USM 100 Shear & Longitudinal Wave Waygate Krautkramer (Formerly GE Inspection)
Equivalent to USMGO in terms of UT testing capability
New capabilities - custom apps and ability to do Encoded Scans along length or circumference
Fully programmable display features and active ultrasonic variables.
Onboard datalogging
Graphic Image Capture & Storage.
Bluetooth communication and interface.

## Slide 29: Mentor UT Phased Array
Phased Array - Sectorial and Linear scans.
Common Applications:
Weld investigation - lack of fusion, porosity, cracks, typically 40°-70°
Castings
Composites
Plastics

## Slide 30: Phased Array Ultrasonic Testing (PAUT) Anatomy
Mode Convergence

## Slide 31: PAUT – Layout ABS-Scans
S-Scan
A-Scan
B-Scan

## Slide 32: RotoArray
Embedded UT transducer and Bladder for C-scan
32/64 elements
Common Applications
Volumetric Flaws –
Flaw based hardness (FBH)
Surface based hardness (SDH)
Porosity
Thickness mapping and measurement
Delamination

## Slide 33: RotoArray(Compact CONT)

## Slide 34: RotoArray(Compact CONT)

## Slide 35: RotoArray(Compact CONT)

## Slide 37: Closing Thoughts
This a Transformative Era
Biggest changes since the Industrial Revolution, beyond the Information Age and Cloud Computing.
Future belongs to those that are first to recognize, adapt and pivot.
Woody Kuntz, 1996
This Photo by Unknown Author is licensed under CC BY

## Slide 38: Questions & Answers

## Slide 39: +
Creative Commons Licenses